LulzBot Filament Testing Report

Manufacturer: ESun
Filament Type:	(PVA)
Tested By:	M. Rosenhagen
Date:	9/28/17

Ease of use:	6/10 I had to adjust the default settings in cura2 to get the print to print ok.
Appearance:	6/10	PVA doesn’t stick well to Polyflex. PVA comes loose while printing on Polyflex.

Color consistency:	10/10

Print temperature Range (C): 180-190 C is recommended. Tried printing at 225 C and the filament started to smoke, may do ok at 200 C but should be kept around 180-190 C.

Variance in diameter:

Minimum bend radius:

Prints using current Lulzbot profiles/temps:

1. “First print” 190C with 175C standby temp.
2. “First print” 200C with 190C standby temp

General Notes:	(Be as detailed as possible)

- Does not stick well to Polyflex
- When PVA is done being used the temp goes down to 0C
- PVA seems to warp, could be from residual glue on bed
Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Health or environmental risks:
See SDS for information.

Disposal Options:

Recommendation:	Use standard PVA settings

Filament disolving:

Revision History

Revision Date	Modifications or Additions	Updated By