LulzBot Filament Testing Report

Manufacturer:	Breathe-3DP
Filament Name:	PLA++
Filament Type:	PLA
Tested By:	Brent M
Date:	01/12/2016

Ease of use:	5/10
Appearance:	8/10
Color consistency:	10/10
Print temperature Range (C):
Melting Point (C): 240 – 260°C
Decomposition Temperature (C): 300°C
Variance in diameter: (2.82-2.85)
Minimum bend radius: NA, extremely ductile
Prints using current Lulzbot profiles/temps: Ooh yeah :) default PLA settings look great

General Notes:
- Currently comes in 6 colors
- Came in a Mylar resealable bag, nice for nylons
- Feels similar in stiffness to Alloy 910
- Prints fairly well using ABS profile with the bed dropped to 70 and the temp at 250
- Spools are labeled with an ID number
- Printed parts do much better than PLA/PHA on overhangs

Health Risks:

Eyes: No significant eye irritation or eye toxicity during normal use.
Skin: No significant skin irritation. Molten polymer may cause thermal burns.
Ingestion: May cause irritation to the throat, mouth and stomach and / or may cause nausea.
Inhalation: Inhalation of process fumes and vapors may cause irritation in the respiratory	system.
Chronic: No known chronic health effects

Environmental Risks:

Ecotoxicity: No information available.
Persistence and degradability: No information available.
Bioaccumulative potential: No information available.

Disposal Options:

Dispose of this product in accordance with local, state and federal regulations.

Recommendation: This filament is LulzBot approved, we should definitely consider this company as a PLA supplier. Size and color consistency are great, and it prints like good PLA should. They sell thins on their site for $48/kg, so it would be more of a village plastics PLA competitor than an eSun replacement.