How to print with ABS

ABS is a combination of Acrylonitrile, butadiene and styrene, and is one of the most comonly used plastics (think lego's, lunchboxes, etc.)

Pros:
- Relatively high glass transition temperature (rigid below ~105C)
- Adheres to itself well, so high printing speeds (~100mm/s) are possible
- Parts can be easily polished and strengthened with acetone washing
Cons:
- Has a high level of thermal expansion so parts shrink after printing, causing warping and cracking
  - Enclosing your printer will help minimize warping, and adding a 2-4mm brim to the part (in slic3r) will prevent lifting at the corners of the part.
- Requires a heated bed, PET tape and ABS/acetone glue to stick to print bed
- Has a mild acrid smell

Nozzle Temperature:	225-235 C (230 default)
Bed Temperature:	85-110 C (85 default)
Nozzle sizes:	.25-1.5mm

Sample Configuration:
These are the settings we use to print the corner pieces that hold the y-rods, these are pretty fast but	produce nice looking, strong parts.

; layer_height = .3125
; perimeters = 2
; top_solid_layers = 4
; bottom_solid_layers = 3
; fill_density = 0.74
; perimeter_speed = 100
; infill_speed = 110
; travel_speed = 160
; nozzle_diameter = 0.5
; filament_diameter = 2.89
; extrusion_multiplier = 1
; perimeters extrusion width = 0.56mm
; infill extrusion width = 0.60mm
; solid infill extrusion width = 0.55mm
; top infill extrusion width = 0.48mm
; first layer extrusion width = 0.58mm