How to print with Thermoplastic Urethane

Thermoplastic urethane (TPU) is a highly elastic plastic that is commonly used to make belts, gaskets and inflatable products. It's combination of shear strength, low temperature performance, abrasion resistance and flexibility make it a very exciting material.

The flexibility of this material makes it nearly impossible to print using a standard extruder (it's like pushing a long rubber band through a straw). Because of this we've designed the Flexystruder, a greg's wade style extruder that fully constrains the filament. We're working on bringing this into our store as a kit, but until then you can make your own following the instructions posted here.

Pros:
- Extrudes well @ 230C and bonds well to ABS for prints that combine rigid and flexible components
- Incredibly strong, a .3mm printed sheet (1 layer) stretches well but is very difficult to tear
- Adheres to itself well, so parts don't de-laminate easily
- The stretchiest material that we've ever tested
- Sticks well to most print surfaces
Cons:
- Requires a modified extruder to print
- Requires relatively low print speeds (30 mm/s)
- More expensive that standard printing materials (~2X ABS/PLA cost)

Nozzle Temperature:	200-230 C (215 default)
Bed Temperature:	0-70 C (60 default)
Nozzle sizes:	.35-1.5mm

Sample Configuration:
Printing with TPU is a bit different than printing with rigid materials like ABS and PLA. The TPU will compress quite a lot between the extruder and nozzle, so you'll have far less control over the feedrate (after you stop extruding, material will continue to feed until the pressure in the nozzle drops). Because of this, you'll want to just try to keep the feedrate constant. To do this you should set ALL speeds (including first layer speed) to the same value between 30mm/s and 40mm/s, with travel set as high as your printer can handle (150mm/s) and retraction bumped up to ~5mm

; layer_height = .3
; perimeters = 3
; top_solid_layers = 3
; bottom_solid_layers = 3
; fill_density = .4
; perimeter_speed = 30
; infill_speed = 30
; travel_speed = 150
; nozzle_diameter = 0.35
; filament_diameter = 2.89
; extrusion_multiplier = 1.4
; perimeters extrusion width = 0.35mm
; infill extrusion width = 0.35mm
; solid infill extrusion width = 0.35mm
; top infill extrusion width = 0.35mm
; first layer extrusion width = 0.35mm