LulzBot Filament Testing Report

Manufacturer: Push Plastics
Filament Type: PC PBT
Tested By: Angelica Nolen
Date:	10/27/2017

Ease of use: 7/10
Appearance: 8/10
Color consistency: 10/10
Print temperature Range (C): (235-255c)
Variance in diameter: (2.85-2.89)
Minimum bend radius: no minimum
Prints using current Lulzbot profiles/temps:
Tested using ABS – IC3D profiles - (230-250°C)

General Notes:	(Be as detailed as possible)
- Packaging: sealed plastic, no issues.
- Melting point, per manufacturer: 200-280°C
- Flash point, per manufacturer: >400°C
- Decomposition, per manufacturer >380°C – Do not print at or above this temperature
- Filament very sensitive to cooling settings, high fan speeds and high minimum layer times can result in poor layer adhesion.
- very pliable
- When filament reel is exposed to a humid environment the resulting print is weak (tested at standard layer height)
- Printing temperature range: 235-255°C
- Bed temperature range: 110-120°C
- Use higher layer heights for best results
- Not for larger scale parts, heated environment required for large prints (Unable to print large scale parts in an open environment )

Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)

Include high strength, high speed, and standard. High Detail not recommended.

Health or environmental risks:

Decomposition products include: carbon monoxide, carbon dioxide, Trace amounts of acrolein, formaldehyde, aldehydes, acids, ketones, and other unidentifiable organic compounds may be formed.

Disposal Options:

The pellets, regrind, and purge of this material are non-hazardous and may be discarded in accordance with state, federal, and local regulations.

Recommendation:	(As thorough as possible)
- Recommended only for small scale parts, larger walls produce cracking in an open air environment when part is larger than a regular soda can (approximately), good for small components only.
- Not highly recommended for beginner customers

Revision History

Revision Date	Modifications or Additions	Updated By
06.28.17	Document Created	J. Pettit
10.27.2017	Data and Recommendations	A. Nolen