LulzBot Filament Testing Report

Manufacturer: Village Plastics
Filament Type: Hips 3
Tested By: Angelica Nolen
Date: 10/31/2017

Ease of use: 9/10
Appearance: 10/10
Color consistency: Cloudy Opaque White (slight pearl shimmer) – UPDATE: PRINT PRODUCT YELLOWS WITH AGE (*the filament on the reel does not appear to change color over time, the printed result changes with the age of the filament being used to print with, the change is not seen until after the model has been printed with the older filament)
Print temperature Range (C):
Variance in diameter: 0.06 mm variance (max)
Minimum bend radius: no minimum
Current Lulzbot profiles/temps Used for Tests:
Village Plastics – Hips (old profile)
General Notes:
- Packaging: vacuum sealed in clear plastic, non resealable
- Bed Temp Increased for adhesion during first run with pre-made profile
- no filament inconsistencies or debris
- When bending, becomes a more opaque white and looses rigidity, rendering it more pliable under stress
- small geometric overhangs exhibit high amounts of overhang/bridging shrinkage debris
- D-limonene results:
- **INCONSISTENT PRINT COLOR OVER TIME – Opened reel used and left in room temperature storage container for 3 months, no abnormal humidity or light exposure during this time.
Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)
All profile levels usable: High Speed, High Detail, and Standard
Health or environmental risks:
- Decomposition temp at 300C
- Flashpoint: 345-360 C
- Non-Toxic
- Not biodegradable
- Keep away from bodies of water and sewers (and drains?)
- Avoid contact with eyes
- Soluble in organic solvents
Disposal Options:
DO NOT ATTEMPT TO DISPOSE OF BY UNCONTROLLED IGNITION.
- This material and its container must be disposed of in a safe way. Dispose of surplus and non-recyclable products via a licensed waste disposal contractor. Disposal of this product, solutions and any by-products should at all times comply with the requirements of environmental protection and waste disposal legislation and any regional local authority requirements.
- The recommended disposal methods for polymers in order of preference are: 1) clean and reuse if possible; 2) contact resin broker; 3) contact plastic recycler; 4) incinerate with waste heat recovery and/or 5) landfill. Reuse, recycling, storing, transportation and disposal must be in accordance with applicable federal, state/provincial and local regulations.
Recommendations:
REJECTED – Inconsistent Print Color with Age

Revision History

Revision Date	Modifications or Additions	Updated By
11/07/17	Data	A. Nolen
03/02/2018	Confirm test profiles and quality	A. Suiter