LulzBot Filament Testing Report

Manufacturer: Biofila
Filament Type: Linen
Tested By: Patrick
Date: 5/5/16

Ease of use:	8/10
Appearance:	9/10
Color consistency:	10/10
Print temperature Range (C):	185-220C
Material Physical Properties:
Melting point / range: 180-235°C
Ignition temperature: not tested
Decomposition temperature: 240°C
Variance in diameter: (2.70-2.80)
Minimum bend radius: Under 1 mm
Prints using current Lulzbot profiles/temps: Prints well enough using default pla profile. It didnt do great with overhangs/bridging and may benfit with its own profile at a lower temperature.

General Notes:
- It looks like dull pla but does not print as well as pla.
- Prints ok with default pla profiles.
- Color was very consistent throughout the roll.
- The cardboard reels are not my favorite.
- Previously we had a hard time purging this material, it seems to not be a problem anymore now.

Health or environmental risks:

Under normal conditions the processing and compounding is stable and there are no observable
hazardous reactions nor products of decomposition.
No toxicologic short-term or long-term effects are known.
The material is only composed of eco-friendly components. So the material can be count as eco-friendly.

Disposal Options:

The best way of disposal is
I.) Recycling, i.e. recovery of the material or
II.) brun, with due regard to the local laws and regulations

Recommendation:
I think the other two filaments from Biofila have more appeal than this one. The parts don't look as cool as the silk and the filament performs worse than their platec. I havent thought of anything useful that you could do with a linen filament print.