LulzBot Filament Testing Report

Manufacturer: Two Bears
Filament Type: bioFila plaTec
Tested By: Patrick
Date: 4/25/16

Ease of use:	10/10
Appearance:	9/10
Color consistency:	10/10
Print temperature Range (C):	185C-220C
Material Physical Properties:
Melting point / range: 160-230C
Ignition temperature: not listed
Decomposition temperature: not listed
Variance in diameter: (2.80-2.85)
Minimum bend radius: Under 6mm was not able to get this to snap easily.
Prints using current Lulzbot profiles/temps: Yes prints great using standard pla profiles.

General Notes:
- This pla is more durable on the reel than most of the other pla filaments we have tested.
- Is expensive and only avalible in natural color.
- Color consistent throughout the roll.
- It looks like they stamped the wrong experation date on the reel then tried to correct it with a ball point pen.
- Printed parts behave like abs when broken rather than shattering like most pla.

Health or environmental risks:

Under normal conditions the processing and compounding is stable and there are no observable
hazardous reactions nor products of decomposition.
No toxicologic short-term or long-term effects are known.
The material is only composed of eco-friendly components. So the material can be count as eco-friendly.

Disposal Options:

The best way of disposal is
I.) Recycling, i.e. recovery of the material or
II.) brun, with due regard to the local laws and regulations

Recommendation:
Filament itself is great, prints are durable, bridging/overhangs look awesome. Reel was mislabled and then fixed with ball point pen, looks a little unprofessional. Overall I would recommend this filament assuming the little cosmetic things on the reel were fixed so that it would be presentable to a customer.