LulzBot Filament Testing Report

Manufacturer: Chromastrand Labs
Filament Type: PETG
Tested By: Angelica Suiter
Date: 12/27/2017

Ease of use: 10/10
Appearance: 10/10
Color consistency: No Variance
Print Temperature Range (C): 215-250 C
Bed Temperature Range (C): 65-75 C
Variance in diameter: 0.04-0.08mm Variance
Minimum bend radius: No Snap Point - 20mm safe bend radius before deformation
Current Lulzbot profiles/temps Used for Tests:
nGen profiles used as base
General Notes:
- easy to print with
- wide print temp range
- flexible material
- Packaging: plastic sealed bag in box, no moisture absorption packet in bag with filament.
- Diameter: 2.85mm (+-0.08)
- 20mm safe bend radius
- Sticks to bed at 65 C, never go above 79 C for bed.
- Moisture test showed little change in print result, small increase in brittle from high levels of moisture exposure (92% humidity for at least 24 hours)
- Extruded at 290 C, no bubbling at higher temps, just a thinner extrusion.
- Starts oozing around 240 C
- Auto ignition temp: decomp 454 C
- Consistent in color and texture, no debris found.
- **Occasionally there is cracking and breaking of the lower layers of a part, I think this has two reasons: 1- the heating and cooling and heating and cooling of the material in the tool head (petg does not reuse well, heating, cooling and reheating inside the tool head can cause the material to become more brittle – considering a large skirt purge amount for production slices) and 2- when the part is being removed, if the removal blade nicks the part and begins a small break, it is highly likely to follow that break (like opening a chip bag, cut one edge and let the tear follow the path)
- The brittle lower layers happen more often (still very rare) on the old one piece beds, I believe this is simply do to the inconsistence of the coils in the bed type, with the two piece beds the changes in temp is always gradual and consistent.
- Packaging: Vacuum sealed inside a plastic bag, bag not reusable and not sealed with moisture absorbing packet. Bag and reel inside box, box is wrapped in a plastic packaging.
Recommended Print Profiles: (ie. should we include high clarity, high strength, etc.)
- High Speed – works well, strong
- Standard – Works well, nice detail, strong
- High Detail – undetermined, encountered a number of issues when trying to get 0.2mm layer height and smaller. Further testing is required.
Health or environmental risks:
- Do not eat.
- Do not touch molten material
- Nothing else of notation known at this time, this is a highly used type of material.
Disposal Options:
In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container.
Recommendation:
- Recommended.
- Prints well, strong and flexible.
- **Concern about brittle material if heated and cooled inside nozzle before use in print. (increase skirt - purge fix?)
Revision History

Revision Date	Modifications or Additions	Updated By
12/27/2017	Testing Update	A. Suiter
01/03/18	Update	A. Suiter