LulzBot Filament Testing Report

Manufacturer:	Smart Materials 3d / enye labs
Filament Name:	b-pet
Filament Type:	recycled PET
Tested By:	Brent M
Date:	03/15/2016

Ease of use:	X/10
Appearance:	7/10
Color consistency:	9/10
Print temperature Range (C):	245-260 (SDS softening 170F)
Variance in diameter: (2.80-2.83)
Minimum bend radius: N/A
Prints using current Lulzbot profiles/temps: No

General Notes:
- Packaged on a colorfabb style clear spool with nice label. Spool was dirty inside of the sealed plastic bag.
- The material still has a very narrow print range, seems to do best at 250C
- Color is pretty consistent
- 1 of 3 prints successful with default profile, slowing down print doesn't seem to help
- Material became noticably clouded after 1 week in r&d
- Seems to do well with INOVA profile with extruder temp bumped up to 250C with a freshly opened reel
- Certain layers turn cloudy white during printing, seems to be related to back-pressure (shows up on overfilled/squished layers

Health or environmental risks:

Threshold Limit Value (TLV): Not established
Emergency and First Aid: If burned by contact with molten material, cool quickly as possible with water, and then go to see a physician for treatment of burn.
Exposure effects:
 Inhalation: No data available
Eyes: Can cause mechanical irritation
May be harmful by ingestion, causes eye and skin irritation

None of the components present in this material at concentrations equal to or greater than 0.1% are listed by IARC, NTP, OSHA or ACGIH as a carcinogen.

Disposal Options:

Recycle, landfill, or incineration. Observe regulations of local authority.

Transportation: This material is NOT classified as dangerous for transport

Recommendation: