Iwatani Filament testing notes:

Notes:
PLA 11
- There was some stripping of the filament when printing at high speeds.
- Sticks almost to good to the bed I had difficulty removing the part.
- The part looks awesome and feels very solid.
- The filament diameter is consistent throughout the reel.
- PLA 11U
- This one also reminds me of t-glass a little bit.
- Seems to be stronger and more rigid like the PLA 12U.
PLA 12U
- This stuff prints awesome and is clearest of the three filaments tested.
- It doesn't strip as easily as the PLA 11.
- This has the most consistent diameter of the three filaments from the company.
PLA 12
- This stuff prints similar to PLA 12U.
- The only difference in this filament vs the others was the sharpie seemed to bleed.
Recommendation: .
All four filaments printed well and were consistent throughout the reel. My favorite was the PLA 12U. The PLA 12 and 12U looked like t-glass but printed like PLA which was awesome.

Filament diameter accuracy / consistency:

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
PLA 11	1.70-1.75 (.02mm)	0.02mm (1.73-1.75)	185C (printed with .4 nozzle)
PLA 11U	1.71-1.73(.02mm)	.01mm (1.72-1.73)	185C (printed at 190C with .4 nozzle)
PLA 12U	1.70-1.71 (.01mm)	0.01mm (1.70-1.71)	185C (printed with .4 nozzle)
PLA 12	1.67-1.77 (.10mm)	0.02mm (1.75-1.77)	185C (printed with .4 nozzle)
Average	1.71mm (+/- .043mm)	0.016mm (1.73)