LulzBot Filament Testing Report

Manufacturer: PolyMaker
Filament Type: PETG
Tested By: Josh W and A. Suiter/Nolen
Date: 12/13/17

Ease of use: 10/10
Appearance: 10/10
Color consistency: 10/10
Print temperature Range (C): (215-250 C)
Bed temperature Range (C): (65-75 C)
Variance in diameter: (2.81-2.91mm)
Minimum bend radius: no snap point, 20mm bend radius before deformation
Prints using current Lulzbot profiles/temps: Polymaker polylite PLA (change temp to 230 hot end and 80 bed) (update 12/13/17 – nGen Colorfabb with edits)

General Notes:	(Be as detailed as possible)
- Printing temperature: 215-250C (230 C Recommended)
- Thermal Decomposition >350°C, do not print at or above this temperature
- 2.85mm (+-.06mm)
- Starts oozing at 225 C
- Consistent color and texture, no debris found.
- 20mm safe bend radius before deformation
- Extruded at 290 C, no bubbling
- Stuck to bed at 65 C - manufacturer recommended bed temp: 80-90C - I recommend keeping the bed temp about 70 C and never above 79 C.
- Do not exceed specified bed temp- could compromise strength of lower layers.
- Packaging: Packed in a box inside of a vacuum sealed plastic bag. Bag is resealable and reusable. Also contained one moisture absorbing bead packet. Box is of high quality and can be used to store filament reals neatly.
- Moisture tests: Cosmetic issues when exposed to 99% Humidity for 24 hours. (this level of exposure is unlikely)
- Their shade of gray is closer to a sea foam green, there have been many comments about loving that color however so instead of adjusting the mix maybe they can rename it? Its very pretty.
- **Occasionally there is cracking and breaking of the lower layers of a part, I think this has two reasons: 1- the heating and cooling and heating and cooling of the material in the tool head (petg does not reuse well, heating, cooling and reheating inside the tool head can cause the material to become more brittle – considering a large skirt purge amount for production slices) and 2- when the part is being removed, if the removal blade nicks the part and begins a small break, it is highly likely to follow that break (like opening a chip bag, cut one edge and let the tear follow the path)
- The brittle lower layers happen more often (still very rare) on the old one piece beds, I believe this is simply do to the inconsistence of the coils in the bed type, with the two piece beds the changes in temp is always gradual and consistent.

Recommended Print Profiles: High detail, standard and high speed, maybe high strength
High Speed – Great, prints neat and strong
Standard – Great, strong and good for detail
High Detail – issues st 0.2mm or smaller layers

Health or environmental risks:
No hazardous Classification
Do Not Eat
Do not touch molten material

Disposal Options:
In accordance with local and national regulations. Do not contaminate ponds, waterways or ditches with chemical or used container.

Recommendation: Good filament, easy to use. Great for accurate cosmetics. Sticks well to the bed. (**note concern about lower layers being brittle, and consider skirt purge fix)

Revision History

Revision Date	Modifications or Additions	Updated By
04.27.17	Created initial document	J. Pettit
07.06.17	Tested filament	J. West
12.13.17	Testing Update	A. Suiter/Nolen

01.03.18	Update	A. Suiter/Nolen