LulzBot Filament Testing Report

Manufacturer:	Proto Pasta
Filament Name:	Black conductive PLA 3.0mm
Filament Type:	Conductive PLA
Date:	3/4/2015

Ease of use:	10/10
Appearance:	looks just like black PLA, a bit matte at standard PLA temps
Size consistency:	Average
Color consistency:	Good
Print temperature:	205/60 (LulzBot Mini)
Prints using Lulzbot profiles/temps: Yes, could use some minor tweaks

Recommendation: This stuff is great. It's more conductive than either of the esun conductive materials I've tested, it prints like PLA should, and it's got an MSDS. Great looking print first time with no noticable effects from the conductive additive.
Notes:
- Prints well with default PLA settings
- Wipe works reasonably well, could be made better with custom config
- Diameter consistency was average
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
3.0mm conductive PLA	2.82-2.89 (.07mm)	0.04mm (2.85-2.89)	190-220C (printed at 205C with standard Mini profiles)