LulzBot Filament Testing Report

Manufacturer:	Toner Plastics
Filament Name:	Red PLA 2.88mm, Lot # 77274
Filament Type:	Opaque red pla
Date:	1/2/2015

Ease of use:	9/10
Appearance:	Good, dull surface at standard Lulzbot print temps
Size consistency:	Average
Color consistency:	No variance
Print temperature:	205/60 (LulzBot Mini)
Prints using Lulzbot profiles/temps: Yes

Recommendation: This PLA prints great at our with our standard print profiles. The extrusion consistency was average, but more recent samples of TP PLA are much more consistent.

Notes:
- Prints well using standard PLA settings
- Nice color, would like to see some translucent PLA from them
- Very little stringing
- Seems like it should be printed at a hotter temperature than our current PLA, but does fine at the default settings
Filament	Variance in diameter	Maximum out of round	Extrusion temperature
2.88mm PLA / Batch # 77274	2.81-2.96 (.15mm) / Note: More recent samples are much better	0.07mm (2.84-2.91)	190-210C (printed at 205C with standard Mini profiles)