LulzBot Filament Testing Report

Manufacturer:	Toner Plastics
Filament Name:	3.0mm Copper PLA Natural
Filament Type:	Copper colored PLA
Date:	2/11/2015

Ease of use:	9/10
Appearance:	Great
Size consistency:	Great consistency
Color consistency:	Very good
Print temperature:	205/60
Prints using Lulzbot profiles/temps: Yes

Recommendation: I really like this stuff, and I haven't seen another copper colored PLA that looks this good. Might be worth having in the store alongside e-sun PLA.

Notes:
- This stuff looks great, better than a lot of polished bronzefill parts I've seen
- Prints well using standard Mini PLA profiles
- Non-conductive and about the same weight as normal PLA – need to make sure people don't confuse it with metal filled filaments
- Bridges well and doesn't ooze much

Filament	Variance in diameter	Maximum out of round	Extrusion temperature
Copper PLA	2.84-2.91 (.06mm)	0.03mm (2.84-2.87)	180-230C (printed at 230C in .5mm hex nozzle)